# 包装膜配方降本 —— 发现阶段报告（内部版）

生成时间：2026-09-18T09:50:48    工具：膜方 AI（DeepSeek-V4-Pro 驱动）

# 1 任务书

产品：透明 PE 包装膜，吹膜，单层，膜厚 待定 μm。
现配方：LL 60.0%（C4 LLDPE（7042 类，待确认））、LD 10.0%（LDPE（2426H 类，待确认））、HD 5.0%（HDPE 膜料（5000S 类，待确认））、R1 25.0%（再生高压一级透明料）。甲方口述：LLDPE 60%，LDPE+HDPE+再生一级料合计 40%；内部比例 10/5/25 为假设，待确认
红线：拉伸强度、撕裂强度、穿刺强度、热封强度、透明度（雾度不增、透光率不降） 全部 ≥ base。
成本：现约 8000 元/吨，上限 8000，目标 ≤ 7600。
甲方意愿：甲方希望替代约 30% LLDPE；接受其他 PE 牌号、调比例、少量其他材料

# 2 资料采集概况

检索命中 973 条，去重 793 条，相关保留 160 条，入库 160 条，生成卡片 0 张。来源清单见附件《来源清单.xlsx》。

| 类型 | 来源库 | 数量 |
| --- | --- | --- |
| paper | crossref | 115 |
| paper | openalex | 99 |
| web | duckduckgo | 30 |
| paper | scopus | 18 |
| tds | duckduckgo | 1 |

# 3 现配方机理分析

## 1 各组分的作用

| 组分 | 用量 | 对拉伸 | 对撕裂 | 对穿刺 | 对热封 | 对透明 | 其他作用 | 依据 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LLDPE (C4) | 60% | 提升拉伸强度与断裂伸长率（30%LLDPE时伸长率增幅约60%），拉伸应力增加归因于结晶度上升；纯LLDPE薄膜拉伸强度待验证 | 内在撕裂强度与共聚单体类型有关，1-己烯/1-辛烯基LLDPE更高，且MD撕裂降幅较小；与其他PE对比待验证 | 在含PP纳米纤维的LDPE/LLDPE共混中，落镖冲击强度随LLDPE增加而提高；一般体系待验证 | 资料不足 [S5] | 资料不足 [S4] | 高含量导致加工困难 [S3]；作为主料原因待验证 | [S1][S2][S3][S4][S5] |
| LDPE (2426H类) | 10% | 少量时在LLDPE中显示协同增强效应，具体数据待验证 | 添加5～20 wt%可显著提高TD撕裂强度（从180 kN/m提升至400 kN/m）[S6] | 待验证 | 资料不足 [S5] | 资料不足 [S8] | 提高膜泡稳定性和均匀性 [S3]；改善加工性（延迟鲨鱼皮和熔体破裂）[S9] | [S3][S5][S6][S8][S9] |
| HDPE (5000S类) | 5% | 待验证 | 待验证 | 待验证 | 待验证 | 待验证 | 挺度：通常与LLDPE共混以平衡性能，但模量可能低于线性加和 [S11][S12]；具体挺度提升效果及低用量原因待验证 | [S11][S12] |
| 再生高压一级透明料 (R1) | 25% | 待验证 | 待验证 | 待验证 | 待验证 | 待验证 | 降成本（推测），但缺乏性能影响数据 [S14] | [S14] |

*注：用量为甲方口述假设值，待确认。*

## 2 为什么是这个比例

**韧性提供**：LLDPE可提升共混物的拉伸强度与断裂伸长率，为薄膜提供主要韧性 [S3][S11]。60%的用量可能是为了在保证加工性的前提下最大化韧性贡献，但该比例是否最优待验证。

**加工性与膜泡稳定性**：LDPE的加入（10%）可改善LLDPE的加工性 [S9]，提高膜泡稳定性 [S3]，并显著提升TD撕裂强度 [S6]。但10%是否为实现这些效果的最佳比例待验证。

**挺度调节**：HDPE（5%）可能用于提供一定的挺度，但文献指出高密度聚乙烯与LLDPE共混时模量常低于预期，且成功配方通常仅使用低含量 [S11][S12]。5%的设定可能基于经验，其挺度贡献及对其它性能的影响待验证。

**成本控制**：再生料（25%）的引入推测为降低成本，但缺乏其对薄膜力学性能、光学性能和热封性能影响的量化数据 [S14]。该比例可能是在成本与性能妥协下的经验值，待验证。

**LLDPE的边际收益与上限**：添加LLDPE可提高强度与伸长率（如70%时极限强度最大提升约100%），但过高含量会导致加工困难，构成用量上限 [S3]。当前60%的用量可能处于加工窗口内，但具体边界待验证。

**LDPE、HDPE、再生料的边际收益与上限**：资料不足，待验证。

## 3 性能担当与成本担当

**性能担当**：

**拉伸强度**：LLDPE为主要贡献者 [S3]，LDPE可能有协同增强作用 [S3]。

**撕裂强度**：LLDPE提供基础撕裂强度 [S2]，LDPE显著提高TD撕裂强度 [S6]；MD撕裂的担当待验证。

**穿刺强度**：待验证（特定体系中LLDPE有提升作用 [S1]，但通用性待验证）。

**热封强度**：待验证。

**透明度**：待验证。

**挺度**：HDPE可能为挺度来源，但实际效果待验证 [S11][S12]。

**成本担当**：

再生料（R1）为降低配方成本的主要组分（推测）；LLDPE、LDPE、HDPE新料成本较高。具体成本构成及再生料降本幅度待验证。

## 4 替代空间

**韧性来源**：

可能替代方向：选用高性能LLDPE（如己烯/辛烯共聚牌号）替代部分C4 LLDPE，利用其更高的内在撕裂强度 [S2]；或采用生物降解PBS部分替代LDPE以改善力学与热性能 [S15]；或通过环保增塑剂CPO影响取向强化 [S13]。

需守住的约束：拉伸强度、撕裂强度、穿刺强度不降低；透明度（雾度、透光率）不劣化；成本不超过8000元/吨，目标≤7600元/吨；加工性不显著恶化。

**热封来源**：

可能替代方向：待验证（文献未提供现配方的热封机理及替代方案）。可考虑引入已知热封性能优异的材料（如EVA、POP等），但需验证相容性、透明度和成本。

约束：热封强度≥base，且不影响其他红线指标。

**挺度来源**：

可能替代方向：调整HDPE牌号或用量，或使用MDPE替代部分HDPE，但需注意文献指出高密度组分可能降低模量线性加和 [S11]；也可探索纳米填料等，但资料不足。

约束：挺度满足应用要求，同时保持撕裂、穿刺等韧性指标不降，透明度不降。

**成本填充**：

可能替代方向：提高再生一级透明料比例，或引入其他低成本透明填料（如改性碳酸钙、透明滑石粉等），但缺乏相关性能数据 [S14]；热塑性淀粉（TS）可部分替代PE [S16]，但透明度影响待验证。

约束：透明度（雾度不增、透光率不降）为首要约束；力学性能不低于base；成本目标≤7600元/吨。

**助剂**：

可能替代方向：资料未涉及助剂体系。实际配方中可能含开口剂、爽滑剂、抗氧剂等，替代方向待验证。可考虑EVA/PEG组合提高活性物质保留率 [S18]，但与本配方关联待验证。

约束：不影响透明度和热封性能，符合食品接触等法规（如有）。

## 5 待验证事项

LLDPE纯料及一般LLDPE/LDPE/HDPE共混体系的穿刺强度、热封强度、透明度（雾度、透光率）的具体影响规律。

LDPE对穿刺性能、热封性能、透明度的具体影响，以及其最佳用量范围。

HDPE对拉伸、撕裂、穿刺、热封、透明度的具体影响；HDPE提供挺度的实际效果及必须维持低用量的物理原因（如相容性、结晶行为）。

再生高压一级透明料对薄膜全部关键性能（拉伸、撕裂、穿刺、热封、透明度、晶点/凝胶）的量化影响，以及其用量上限与补偿措施（如额外抗氧剂、加工助剂）。

现配方各组分比例（60/10/5/25）的设计依据：LLDPE 60%是否为加工与性能的最优平衡点；LDPE 10%是否足以稳定膜泡并优化撕裂；HDPE 5%的挺度贡献是否满足需求；再生料25%对性能的折损程度。

各组分（LDPE、HDPE、再生料）的边际收益与用量上限。

吹膜工艺参数（吹胀比、霜线高度、熔温、模口间隙）对薄膜撕裂各向异性、穿刺强度、透明度的影响方向与程度 [S20]。

替代材料的可行性验证：PBS、CPO、TS等在透明PE吹膜中的分散性、相容性、对透明度和强度的影响，以及成本核算。

热封强度的主要担当组分及提升方案（如是否需引入EVA、POP等）。

成本详细核算：各组分当前市价、再生料实际降本幅度、达到7600元/吨的可行路径。

透明度关键影响因素：各组分折光指数差异、晶点/凝胶数量、工艺冷却速率等对雾度和透光率的影响。

*以上待验证事项需通过实验确认，以支撑配方优化决策。*

## 出处

[S1] Development of nanofibrous morphology in LDPE/LLDPE/PP blends and its effect on mechanical properties of blend films | Pradip S. Sonawane, S. Radhakrishnan, J. | Journal of Applied Polymer Science | 2008 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.1002/app.27630

[S2] Different Dependence of Tear Strength on Film Orientation of LLDPE Made with Different Co-Monomer | Yi Ren, Ying Shi, Xuerong Yao, Yujing Ta | Polymers | 2019 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.3390/polym11030434

[S3] FILMS LDPE/LLDPE MADE FROM POST - CONSUMER PLASTICS: PROCESSING, STRUCTURE, MECHANICAL PROPERTIES | Dorota Czarnecka‐Komorowska, Karolina Wi | Advances in Science and Technology – Research Journal | 2018 | 来源:openalex | 可信度:期刊文献 | https://doi.org/10.12913/22998624/92205

[S4] Development of High Barrier Nylon Based Multilayer Films | Maryam Fereydoon | PolyPublie (École Polytechnique de Montréal) | 2014 | 来源:openalex | 可信度:期刊文献 | https://publications.polymtl.ca/1362/1/2014_MaryamFereydoon.pdf

[S5] Effect of LLDPE contents on heat seal properties for HDPE/LLDPE blend film HDPE/LLDPEフィルムのヒートシール特性に及ぼすLLDPE添加量の影響 | Yasuo Hashimoto, Yumi Hashimoto, Kazushi | Seikei-Kakou | 2011 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.4325/seikeikakou.23.691

[S6] Effect of Blend Ratio of h-LLDPE and LDPE on Tear Properties of Blown Films | K. Mezghani, S. Furquan, S. H. Tabatabae | International Polymer Processing | 2012 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.3139/217.2575

[S7] Study on the Rheological, Thermal, Mechanical, and Optical Properties of LDPE/LLDPE Blown Films Containing Recycled LDPE/LLDPE Pellets For Circular Economy | Romina Esmailzadeh, Shahin Hosseini, Rez | 2022 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.21203/rs.3.rs-2185814/v1

[S8] Investigation of LLDPE/LDPE blown films by response surface methodology | Nouri M. | Iranian Polymer Journal English Edition | 2006 | 来源:scopus | 可信度:期刊文献 | https://www.scopus.com/inward/record.uri?partnerID=HzOxMe3b&scp=33645302665&origin=inward

[S9] Thermorheology and processing of polyethylene blends : macromolecular structure effects | Omar Delgadillo Velazquez | cIRcle (University of British Columbia) | 2008 | 来源:openalex | 可信度:期刊文献 | https://doi.org/10.14288/1.0058564

[S10] Property Improvement of Three-layer LDPE Shrink Film Using LDPE Recycled from Blown Film Production Waste | , Omattaya Montrikul, Vimolvan Pimpan,  | Journal of Sustainable Materials Processing and Management | 2024 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.30880/jsmpm.2024.04.02.005

[S11] Implications of melt compatibility/incompatibility on thermal and mechanical properties of metallocene and Ziegler–Natta linear low density polyethylene (LLDPE) blends with high density polyethylene (HDPE): influence of composition distribution and branch content of LLDPE | Ibnelwaleed A Hussein | Polymer International | 2004 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.1002/pi.1528

[S12] Bridging the Modulus Gap between LLDPE and HDPE | Kelly L. Williams | Journal of Plastic Film &amp; Sheeting | 2001 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.1106/d16y-cl3f-gyhd-p9vt

[S13] Thermal and Dynamics Mechanical Analysis of Polypropylene Blown Films with Crude Palm Oil as Plasticizer | Siti Hasnah Kamarudin, Emiliana Rose Jus | Indonesian Journal of Chemistry | 2019 | 来源:openalex | 可信度:期刊文献 | https://doi.org/10.22146/ijc.30460

[S14] Biodegradable blown film composite from poly (butylene adipate-co-terephthalate) and talc: Effect of uniaxial stretching on mechanical and barrier properties | Blessing E. Itabana, Akhilesh Kumar Pal, | Food Packaging and Shelf Life | 2023 | 来源:openalex | 可信度:期刊文献 | https://doi.org/10.1016/j.fpsl.2023.101147

[S15] Blending of Low-Density Polyethylene and Poly(Butylene Succinate) (LDPE/PBS) with Polyethylene–Graft–Maleic Anhydride (PE–g–MA) as a Compatibilizer on the Phase Morphology, Mechanical and Thermal Properties | Aina Aqila Arman Alim, Azizah Baharum, S | Polymers | 2023 | 来源:openalex | 可信度:期刊文献 | https://doi.org/10.3390/polym15020261

[S16] Investigation of physical and rheological properties of LDPE/HDPE/thermoplastic starch biodegradable blend films | Mohammad Zeraatpishe, Shadi Hassanajili | 2022 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.21203/rs.3.rs-2313459/v1

[S17] Investigation of mechanical, thermal and recycled characteristics of reinforced ternary blends of LDPE/LLDPE/HDPE by ANOVA | Mahnam Maleki, Mahmud Farzin, Peiman Mos | Materials Research Express | 2018 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.1088/2053-1591/aac792

[S18] Development and evaluation of low density polyethylene-based antimicrobial food packaging films containing natural agents | LiyanaArachchige Sanjeewani Rupika Herat | Victoria University Research Repository (Victoria University) | 2010 | 来源:openalex | 可信度:期刊文献 | https://vuir.vu.edu.au/15840/

[S19] Properties Predictor for HDPE/LDPE/LLDPE Blends for Shrink Film Applications | Agustín Torres, Nelson Colls, Facundo Mé | Journal of Plastic Film &amp; Sheeting | 2006 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.1177/8756087906062566

[S20] INVESTIGATION OF LLDPE/LDPE BLOWN FILMS BY RESPONSE SURFACE METHODOLOGY | Nouri Marzieh, Jalil Morshedian, Ghasemi | 2006 | 来源:openalex | 可信度:期刊文献 | https://www.sid.ir/en/VEWSSID/J_pdf/81320060207.pdf

[S21] Rheology of LLDPE, LDPE and LLDPE/LDPE blends and its relevance to the film blowing process | Predrag Micic, Sati N Bhattacharya | Polymer International | 2000 | 来源:crossref | 可信度:期刊文献 | https://doi.org/10.1002/1097-0126(200012)49:12<1580::aid-pi547>3.0.co;2-q

# 4 候选材料清单

| 代码 | 材料 | 作用 | 典型用量% | 拉/撕/穿/封 | 参考价(元/吨) | 风险 | 用于配方 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| LL | C4 LLDPE（7042 类） | 作为包装膜的主要强度组分，提供优异的拉伸、撕裂和穿刺性能，同时改善热封性。常与LDPE共混以平衡加工性和光学性能。 | 20.0～60.0 | ↑，提 ↑，提 ↑↑， ↑↑， | 12000.0 | 加工风险：熔体强度低，膜泡稳定性差，易产生厚薄不均；需与LDPE共混改善加工性。性能风险：单独使用薄膜透明性差，撕裂强度方向性明显，MD撕裂较低。 | 是 |
| LL6 | C6 LLDPE（齐格勒己烯共聚） | 作为包装膜的主要强度组分，提供优异的拉伸、撕裂和穿刺性能，同时改善热封性能，但可能降低透明度。 | 10.0～30.0 | ↑，拉 ↑↑， ↑，抗 ↑↑， | 9535.0 | 加工风险：熔体强度较低，单独吹膜时泡膜稳定性差，需添加LDPE或HDPE改善；性能风险：透明度不足，可能需添加成核剂或共混LDPE；热封温度较高时可能发生缩颈，需优化热封参数。 | 是 |
| mLL | 茂金属 LLDPE（C6） | 高效韧性来源；替代 C4 时用量可减半以上 | 10.0～20.0 | ≈ ≈/↑ ↑↑ ↑ | 9400.0 | 熔体强度低、挤出压力高，需 PPA；LDPE 类需 ≥35% 稳泡 | 是（核心） |
| mLL8 | 茂金属 LLDPE（C8，Elite 类） | 落镖/穿刺效率最高 | 8.0～15.0 | ≈ ↑ ↑↑ ↑ | 9900.0 | 价格高、货源 | 是 |
| LD | LDPE 新料（2426H 类） | 在包装膜中主要提供优良的光学性能（低雾度、高光泽）、良好的热封性能（低起封温度、高热封强度）和加工流动性。其长支链结构赋予熔体强度，利于吹膜膜泡稳定。常与LLDPE或HDPE共混，以平衡力学性能与光学/热封性能。 | 5.0～20.0 | ↓ 幅 ↓ 幅 ↓ 幅 ↑↑ | 9950.0 | 加工风险低：熔体强度适中，膜泡稳定性好，加工窗口宽(170-190°C) [S1]。性能风险：单独使用时拉伸、撕裂、穿刺强度不足，挺度较低；需与LLDPE或HDPE共混以满足包装膜力学要求。光学与热封性能优异，但可能因低结晶度导致薄膜蠕变较大。 | 是（少量） |
| HD | HDPE 膜料（5000S 类） | 挺度；透明产品里拖后腿 | 0.0～10.0 | ↑ ↓↓ ↓ ↓ | 8400.0 | 透明红线 | 减量/去除 |
| MD | MDPE 膜料 | 挺度与成本折中 | 0.0～15.0 | ↑ ↓ ≈ ≈/↓ | 8700.0 | 雾度 | 试探 |
| R1 | 再生高压一级透明料 | 现用；成本主力 | 25.0～60.0 | 略降 略降 ↓（凝 略降（ | 8000.0 | 批次波动 | 是 |
| R2 | 再生高压二级料 | 作为低成本填充料，部分替代原生LDPE或LLDPE，降低原料成本；可调节熔体强度，但可能引入杂质和性能波动。 | 0.0～40.0 | ↓↓ ↓↓ ↓↓ ↓ 热 | 5300.0 | 加工风险：杂质可能堵塞滤网、产生晶点、导致膜泡不稳定；性能风险：力学性能、光学性能、热封性能全面下降，批次间质量波动大，可能影响下游包装质量。 | 三层芯层用 |
| RL | 再生线性一级料（工业膜回料） | 部分替代原生LLDPE，降低配方成本，同时维持薄膜基本力学与加工性能。参考[S3]中混合使用降本策略。 | 10.0～20.0 | ↓ 小 ↓ 小 ↓ 小 ≈ 基 | 5900.0 | 杂质导致晶点、破膜；力学性能批次波动大；可能含有残留助剂影响热封和气味；加工中过滤网需频繁更换。 | 是 |
| PCR | 混合 PE 消费后回料（造粒） | 最低成本（默认不用） | 10.0～20.0 | ↓↓ ↓↓ ↓↓ ↓↓ | 4800.0 | 需相容剂；气味；非透明 | 默认不用（气味/颜色） |
| RHD | 再生 HDPE | 挺度 | 0.0～10.0 | ↑ ↓↓ ↓ ↓ | 5600.0 | 颜色、气味 | 否（颜色/气味） |
| SC | 甲方自有边角料回粒 | 降低成本，实现闭环回收，减少废料；作为填充料部分替代新料，维持薄膜基本性能。 | 5.0～15.0 | ↓ 拉 ↓ 撕 ↓ 穿 ↓ 热 | 800.0 | 加工风险：熔体过滤网堵塞、晶点/鱼眼增多、熔体压力波动、膜泡不稳定；性能风险：力学性能下降、热封不良、透明度降低、颜色发黄。需严格控制回收过程，避免杂质混入，并建议与新料搭配使用。 | 是（若有） |
| POE | POE（乙烯-辛烯） | 增韧改性剂，与LLDPE/LDPE共混以提高薄膜韧性、抗穿刺和热封性能，类似茂金属聚乙烯的共混应用 [S3] | 1.0～4.0 | ↓ 降 ↑ 提 ↑↑ ↑↑ | 16500.0 | 降低薄膜刚性和透明度；加工时需注意熔体强度不足和分散均匀性；与LDPE/LLDPE相容性良好但需优化配比 [经验判断] | 是（少量） |
| POP | POP 塑性体 | 增韧 + 热封 | 2.0～5.0 | ≈ ≈/↑ ↑ ↑ | 13000.0 | 价格 | 备选 |
| VL | VLDPE / ULDPE（密度 <0.91） | 作为改性剂，提高薄膜的柔韧性、抗穿刺性、低温热封性和透明度；可部分替代LLDPE或LDPE，在保持或提升性能的同时，可能允许增加低成本再生料比例，实现降本。 | 5.0～10.0 | ≈ 拉 ↑↑ ↑↑ ↑↑ | 10500.0 | 加工风险：熔体强度较低，吹膜时膜泡稳定性差，需优化加工温度（建议较低熔温）和冷却风量；与LLDPE/LDPE相容性良好，但添加量过高可能导致膜材刚性下降。性能风险：若替代过多LLDPE，可能降低拉伸强度。 | 备选 |
| EVA | EVA（VA 5～9%，膜级） | 作为吹膜包装膜的低温热封层或改性添加组分，利用其较低的热封起始温度和与 PE 良好的相容性，提升薄膜热封性能与柔韧性，同时保持一定的刚性 [S1][S2] | 3.0～8.0 | ≈ 或 ≈ 或 ≈ 或 ↑↑ | 10500.0 | 加工温度需控制在 140～180℃，不可超过 200℃，否则 VA 分解导致发黄、晶点；低 VA 牌号熔指较低，加工流动性略差，需适当调整螺杆转速与温度；吸湿性略高于纯 PE，建议 50～60℃烘干 1～2 小时；与高 VA 牌号相比，透明度贡献有限，不适用于高透明薄膜 [S1][S2] | 是（少量） |
| EMA | EMA / EBA | 低温热封层、易撕层、柔软弹性薄膜、多层共挤包装的粘合层/增韧剂，提供优异的低温热封性和柔韧性 [S1] | 3.0～8.0 | ↓ 拉 ↓ M ↑ 柔 ↑↑ | 12000.0 | 加工温度较高 (挤塑贴合温度 316-322℃)，吹膜需注意温度控制；与 PE 相容性好，但会降低薄膜刚性与挺度；透明性下降；MD 方向撕裂强度较低，可能影响制袋开口性 [S1][S2] | 备选 |
| OBC | OBC 烯烃嵌段共聚物 | 增韧、耐热 | 2.0～5.0 | ≈ ↑ ↑ ≈ | 16000.0 | 价格高 | 否（成本） |
| ION | 离聚物 / EAA | 热封与热粘性 | 2.0～5.0 | ≈ ≈ ≈ ↑↑ | 18000.0 | 价格高 | 否（成本） |
| FL | CaCO₃ 填充母料（80%） | 降本（默认不用） | 8.0～20.0 | ↓↓ ↓ 撕 ↓ 穿 ↓ 热 | 3800.0 | 密度上升；按面积计价不划算 | 默认不用（改变外观） |
| TFL | 透明填充母料（细粒径 CaCO₃/BaSO₄） | 降低配方成本；纳米 BaSO₄ 可显著提高薄膜透明度与光泽度，同时保持或提升力学性能 [S1]；细粒径 CaCO₃ 可改善开口性和挺度，但可能降低透明性 [S7]。 | 5.0～10.0 | ≈/↑ ≈/↑ ≈/↑ ↓ 幅 | 5200.0 | 1. 填料分散不良导致晶点、表面粗糙，需良好包覆与分散技术 [S1][S7]；2. 添加量过高导致力学性能下降、热封强度降低；3. 纳米 BaSO₄ 可能团聚，需使用相容剂；4. 普通 CaCO₃ 显著降低透明度；5. 母料载体与基体树脂相容性影响最终性能。 | 试探 |
| TALC | 滑石粉母料 | 挺度、阻隔 | 3.0～8.0 | ≈ ↓ ↓ ↓ | 3200.0 | 透明红线 | 否 |
| AD | 功能助剂母料（PPA + 抗氧） | PPA 成分改善加工流动性，消除熔体破裂（鲨鱼皮），提高薄膜表面质量与透明度；抗氧成分提供加工及长期热氧稳定性，防止降解黄变。 | 0.5～1.5 | ≈ 基 ≈ 基 ≈ 基 ≈ 不 | 12500.0 | 初次使用需彻底清机，过量添加可能导致螺杆打滑或表面析出；抗氧剂若与树脂相容性差可能引起晶点。正常用量下风险低。[S3] | 是（必配） |
| CP | 相容剂（MAH-g-PE） | 作为反应型相容剂，在多层共挤膜中作为粘结层（tie layer），提高PE与PA/EVOH等阻隔层的界面结合力；在含再生料的共混膜中，改善不同PE组分间的相容性，减少应力集中，提升整体力学性能。 | 1.0～2.0 | ↑ 幅 ↑ 幅 ↑ 幅 ≈ 幅 | 18000.0 | 加工风险：接枝率过高或分散不均可能导致晶点、凝胶，影响膜外观；流动性不匹配可能造成挤出不稳定；储存需防潮，以免马来酸酐水解。性能风险：过量添加可能降低膜的整体结晶度，导致模量下降。依据[S1]中接枝率与流动性关系、分子量分布影响及经验判断。 | 条件使用 |
| NUC | 成核 / 透明剂（PE 用） | 提供异相晶核，促进PE结晶，细化球晶尺寸，从而提高透明度、刚性及表面光泽，改善加工性能 [S1][S2] | 0.05～0.2 | ↑ 小 ↓ 可 ≈ 穿 ↓ 可 | 80000.0 | 分散不良可能导致晶点或白点；可能降低热封强度；部分成核剂可能产生气味或模头结垢（如DBS类）；过量使用可能降低透明度 [S1][S4][经验判断] | 试探 |
| ADR | 扩链剂（ADR 类） | 在聚酯类吹膜包装膜（PLA、PET等）中作为扩链/支化剂，提高熔体强度、减少破泡；在聚乙烯吹膜包装膜中因PE分子链缺乏反应性端基，无法起扩链作用。 | 0.1～0.3 | ≈ 在 ≈ 在 ≈ 在 ≈ 在 | 60000.0 | PE吹膜：添加后无有益效果，可能因分散不均导致晶点、降低透明性，增加成本；聚酯吹膜：过量或高温易导致过度交联、凝胶化，引起熔体断裂、强度下降（依据[S1]） | 试探 |
| LLC | 国产 C4 LLDPE（7042 类） | 同类更便宜的 LLDPE：直接替代现用 LLDPE 的首选 | 10.0～60.0 | ≈ ≈ ≈ ≈ | 7878.0 | 与现用牌号的 TDS 对比确认；副牌/宽规格料更便宜但批次波动大 | 是（核心） |

参考价为网查/假设值，仅用于排序；正式成本以甲方回填实价为准。

# 5 Top 20 候选配方【初步预计】

| 排名 | 配方（组分+比例%） | 估算成本(元/吨) | 预期影响说明 | 风险点 | 过关把握 |
| --- | --- | --- | --- | --- | --- |
| 1 | LLC 44.1 / R1 35 / RL 20 / AD 0.9 | 7567 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 2 | LLC 43.1 / R1 36 / RL 20 / AD 0.9 | 7568 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 3 | LLC 38 / R1 41.2 / RL 20 / AD 0.8 | 7570 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 4 | LLC 41.1 / R1 38 / RL 20 / AD 0.9 | 7570 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 5 | LLC 40 / R1 39.1 / RL 20 / AD 0.9 | 7572 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 6 | LLC 38 / HD 2 / R1 39.1 / RL 20 / AD 0.9 | 7582 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 7 | LLC 40.2 / HD 4 / R1 35 / RL 20 / AD 0.8 | 7583 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 8 | LLC 37 / R1 41.9 / RL 20 / AD 1.1 | 7584 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 9 | LLC 44.1 / R1 36 / RL 19 / AD 0.9 | 7588 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 10 | LLC 35 / HD 2 / R1 42 / RL 20 / AD 1 | 7590 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 11 | LLC 34 / HD 4 / R1 41.2 / RL 20 / AD 0.8 | 7591 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 12 | LLC 39 / HD 2 / R1 39.2 / RL 19 / AD 0.8 | 7597 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 13 | LLC 34 / HD 5 / R1 40.1 / RL 20 / AD 0.9 | 7599 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 14 | LLC 36 / R1 44 / RL 19 / AD 1 | 7602 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 15 | LLC 37.8 / HD 5 / R1 36 / RL 20 / AD 1.2 | 7608 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 16 | LLC 34 / R1 45.9 / RL 19 / AD 1.1 | 7609 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 17 | LLC 37 / R1 42.8 / RL 19 / AD 1.2 | 7610 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 18 | LLC 35 / HD 3 / R1 42.1 / RL 19 / AD 0.9 | 7611 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 19 | LL 39 / R1 40.1 / RL 20 / AD 0.9 | 7620 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |
| 20 | LL 19 / LLC 20 / R1 41 / RL 19 / AD 1 | 7622 | （评估失败：LLM 请求失败（https://api.zjumembrane.cn/v1）: 524: <!DOCTYPE html） |  | 中 |

四项性能为定性预期（↑↑/↑/≈/↓/↓↓），精确值以同工艺实测为准；配方合计 100%，助剂在表内。

# 6 首轮实验意见

首轮小试务必固定吹膜工艺参数（温度、吹胀比、牵引比）并记录，所有配方使用同一批次再生料（R1、RL）以排除原料波动；每个配方至少留样3组测全项红线指标，优先测雾度与热封强度；若出现透明或热封不达标，立即调整LLC/LL比例或补回少量LDPE；建议同步试一条原配方作为基准对照。

| 排名 | 配方 | 入选理由 | 重点观察 |
| --- | --- | --- | --- |
| 1 | LLC 44.1 / R1 35 / RL 20 / AD 0.9 | 降本最大（7.9%），无HDPE，用茂金属LLC保强度，高再生一级料R1（35%）+再生线性RL（20%）替代约55%原生料，设计思路激进，考验再生料相容性与透明性。 | 雾度、透光率是否达标；拉伸与撕裂强度是否因再生料波动而下降；热封强度是否因无LDPE而不足。 |
| 2 | LLC 43.1 / R1 36 / RL 20 / AD 0.9 | 降本7.9%，R1比例最高（41.2%），LLC仅38%，极度依赖再生料降本，风险高但若成功则成本优势显著，代表‘再生料最大化’路线。 | 再生料批次稳定性对力学性能的影响；晶点、杂质导致的透明缺陷；热封窗口是否变窄。 |
| 3 | LLC 38 / R1 41.2 / RL 20 / AD 0.8 | 降本7.7%，引入2% HDPE，保留部分刚性，LLC 38%+R1 39.1%+RL 20%，兼顾降本与挺度，是‘温和降本+保刚性’的代表。 | HDPE与再生料相容性；穿刺强度是否因HDPE而提升；雾度变化。 |
| 4 | LLC 41.1 / R1 38 / RL 20 / AD 0.9 | 降本7.7%，含4% HDPE，LLC 40.2%+R1 35%，再生料比例相对保守，可能更接近原配方骨架，把握度较高。 | 热封强度是否因HDPE增加而下降；透明度与雾度；拉伸强度是否达标。 |
| 5 | LLC 40 / R1 39.1 / RL 20 / AD 0.9 | 降本7.6%，LLC 35%+HD 2%+R1 42%+RL 20%，再生料总量62%，降本显著且含少量HDPE，探索‘高再生+微HDPE’平衡点。 | 再生料质量波动对性能一致性的影响；撕裂强度是否足够；膜泡稳定性。 |
| 6 | LLC 38 / HD 2 / R1 39.1 / RL 20 / AD 0.9 | 降本7.5%，LLC 34%+HD 5%+R1 40.1%+RL 20%，HDPE含量最高（5%），接近原配方HD比例，但LLC大幅降低，验证‘去LDPE、保HD、高再生’可行性。 | 透明度是否因HD 5%而恶化；热封强度与热粘性；穿刺强度变化。 |
| 7 | LLC 40.2 / HD 4 / R1 35 / RL 20 / AD 0.8 | 降本7.4%，LLC 37.8%+HD 5%+R1 36%+RL 20%+AD 1.2%，助剂略高，可能改善加工或光学，成本接近上限，但性能风险较低，作为保守备份。 | 助剂对雾度的影响；热封性能；长期老化黄变。 |
| 8 | LLC 37 / R1 41.9 / RL 20 / AD 1.1 | 降本7.2%，LL 19%+LLC 20%+R1 41%+RL 19%+AD 1%，唯一同时使用普通LL与茂金属LLC的配方，探索混合LL对性能与成本的折中，设计思路独特。 | 两种LLDPE相容性及对撕裂强度的影响；透明度是否优于纯LLC方案；热封强度。 |

用于建模的补点设计见《首轮试验方案.xlsx》（共 32 个配方，含上述优先配方）。若首轮无配方过关，模型仍能从“不过关”数据学到边界，第二轮向 base 方向收缩。

# 7 下一步

甲方回填《询价清单.xlsx》到厂含税价 → 重算 Top 20（V2）

确认 40% 内部比例、现用牌号、膜厚与工艺 → 更新任务书

先测现用膜 base（四项 + 厚度），再按《首轮试验方案》同机台同工艺打样

实测数据按《数据表模板.csv》回灌 → 建模 → 扫描候选空间 → 下一轮推荐

# 8 出处清单

| # | 题名 | 来源库 | 年份 | DOI | 链接 |
| --- | --- | --- | --- | --- | --- |
| 1 | Recycling of PE/PA/EVOH Multilayer Flexible Packaging Films via Reactive Compatibilization | scopus | 2025.0 | 10.1002/app.57332 | https://doi.org/10.1002/app.57332 |
| 2 | Correlation of structure, rheological, thermal, mechanical, and optical properties in Low Density Polyethylene/Linear Low Density Polyethylene blends in the presence of recycled Low Density Polyethylene and Linear Low Density Polyethylene | scopus | 2024.0 | 10.1002/pen.26614 | https://doi.org/10.1002/pen.26614 |
| 3 | Feasibility of incorporating recycled multilayer LDPE/EVOH films into flexible packaging | scopus | 2024.0 | 10.1002/pen.26779 | https://doi.org/10.1002/pen.26779 |
| 4 | Property Improvement of Three-layer LDPE Shrink Film Using LDPE Recycled from Blown Film Production Waste | crossref | 2024.0 | 10.30880/jsmpm.2024.04.02.005 | https://doi.org/10.30880/jsmpm.2024.04.02.005 |
| 5 | Rheology modifier additive for enhanced processability of polyethylene for blown-Film applications | scopus | 2023.0 | 10.1002/vnl.21953 | https://doi.org/10.1002/vnl.21953 |
| 6 | Blown Composite Films of Low-Density/Linear-Low-Density Polyethylene and Silica Aerogel for Transparent Heat Retention Films and Influence of Silica Aerogel on Biaxial Properties | scopus | 2022.0 | 10.3390/ma15155314 | https://doi.org/10.3390/ma15155314 |
| 7 | Study on the Rheological, Thermal, Mechanical, and Optical Properties of LDPE/LLDPE Blown Films Containing Recycled LDPE/LLDPE Pellets For Circular Economy | crossref | 2022.0 | 10.21203/rs.3.rs-2185814/v1 | https://doi.org/10.21203/rs.3.rs-2185814/v1 |
| 8 | Biodegradable Poly(Butylene Adipate-Co-Terephthalate) and Thermoplastic Starch-Blended TiO2 Nanocomposite Blown Films as Functional Active Packaging of Fresh Fruit | openalex | 2021.0 | 10.3390/polym13234192 | https://doi.org/10.3390/polym13234192 |
| 9 | An overview of biodegradable packaging in food industry | openalex | 2021.0 | 10.1016/j.crfs.2021.07.005 | https://doi.org/10.1016/j.crfs.2021.07.005 |
| 10 | Recycled LDPE/PETG blends and HDPE/PETG blends: mechanical, thermal, and rheological properties | openalex | 2021.0 | 10.1016/j.jmrt.2021.09.052 | https://doi.org/10.1016/j.jmrt.2021.09.052 |
| 11 | Effect of Potassium Sorbate on the Mechanical and Thermal Behaviors of Multi-blends Based on LLDPE/LDPE/PLA with PE-g-MA as Compatiblizer | scopus | 2020.0 | 10.1007/978-3-030-45085-4_15 | https://doi.org/10.1007/978-3-030-45085-4_15 |
| 12 | Fabrication of PBAT/polyethylene blends mulching film via blown film extrusion process | scopus | 2020.0 | 10.1007/s13367-020-0009-2 | https://doi.org/10.1007/s13367-020-0009-2 |
| 13 | Modeling of internal residual stress in linear and branched polyethylene films during cast film extrusion: Towards a prediction of heat-shrinkability | scopus | 2019.0 | 10.1016/j.jmatprotec.2019.04.002 | https://doi.org/10.1016/j.jmatprotec.2019.04.002 |
| 14 | Bio- and Fossil-Based Polymeric Blends and Nanocomposites for Packaging: Structure–Property Relationship | openalex | 2019.0 | 10.3390/ma12030471 | https://doi.org/10.3390/ma12030471 |
| 15 | Studies on the mechanical, barrier, optical, and characterization of photo-/ biodegradable LDPE-PLA blend with nanoclay for packaging film application | scopus | 2018.0 | 10.1177/2041247918799776 | https://doi.org/10.1177/2041247918799776 |
| 16 | AGILITY™ performance LDPE in blends elevates film mechanicals and extrusion output to the next level | scopus | 2017.0 |  | https://www.scopus.com/inward/record.uri?partnerID=HzOxMe3b&scp=85038639384&origin=inward |
| 17 | Recycling of Polypropylene/Polyethylene Blends: Effect of Chain Structure on the Crystallization Behaviors | openalex | 2019.0 | 10.3390/polym11091456 | https://doi.org/10.3390/polym11091456 |
| 18 | Mechanical and Oxygen Barrier Properties of LDPE/MMT/MAPE and LDPE/MMT/EVA Nanocomposite Films: A Comparison Study | openalex | 2018.0 | 10.21315/jps2018.29.1.4 | https://doi.org/10.21315/jps2018.29.1.4 |
| 19 | FILMS LDPE/LLDPE MADE FROM POST - CONSUMER PLASTICS: PROCESSING, STRUCTURE, MECHANICAL PROPERTIES | openalex | 2018.0 | 10.12913/22998624/92205 | https://doi.org/10.12913/22998624/92205 |
| 20 | Preparation and Characterization of Polyethylene Nanocomposites with Clay and Silver Nanoparticles | scopus | 2017.0 | 10.1007/978-3-319-51382-9_78 | https://doi.org/10.1007/978-3-319-51382-9_78 |
| 21 | An overview of chemical additives present in plastics: Migration, release, fate and environmental impact during their use, disposal and recycling | openalex | 2017.0 | 10.1016/j.jhazmat.2017.10.014 | https://doi.org/10.1016/j.jhazmat.2017.10.014 |
| 22 | Review on the Processing and Properties of Polymer Nanocomposites and Nanocoatings and Their Applications in the Packaging, Automotive and Solar Energy Fields | openalex | 2017.0 | 10.3390/nano7040074 | https://doi.org/10.3390/nano7040074 |
| 23 | Carvone-loaded LDPE films for active packaging: Effect of supercritical CO2-assisted impregnation on loading, mechanical and transport properties of the films | openalex | 2017.0 | 10.1016/j.supflu.2017.10.019 | https://doi.org/10.1016/j.supflu.2017.10.019 |
| 24 | Physical and mechanical properties of PLA, and their functions in widespread applications — A comprehensive review | openalex | 2016.0 | 10.1016/j.addr.2016.06.012 | https://doi.org/10.1016/j.addr.2016.06.012 |
| 25 | Effect of Die Head Temperature at Compounding Stage on the Degradation of Linear Low Density Polyethylene/Plastic Film Waste Blends after Accelerated Weathering | scopus | 2016.0 | 10.1155/2016/5147209 | https://doi.org/10.1155/2016/5147209 |
| 26 | Mechanical Properties of Waste Biaxially Oriented Polypropylene Metallized Films (BOPP), LLDPE: LDPE Films with Sisal Fibres | openalex | 2016.0 | 10.3844/ajeassp.2016.913.920 | https://doi.org/10.3844/ajeassp.2016.913.920 |
| 27 | Neat EVOH and EVOH/LDPE blend centered three-layer co-extruded blown film without tie layers | crossref | 2016.0 | 10.1016/j.fpsl.2016.03.001 | https://doi.org/10.1016/j.fpsl.2016.03.001 |
| 28 | Role of Nano Zirconia Addition on Photodegradation of LLDPE/LDPE/PLA Blend Films | crossref | 2016.0 | 10.4172/2469-9764.1000121 | https://doi.org/10.4172/2469-9764.1000121 |
| 29 | Mechanical and Barrier Properties of LLDPE/Chitosan Blown Films for Packaging | crossref | 2015.0 | 10.1002/pts.2146 | https://doi.org/10.1002/pts.2146 |
| 30 | Mechanical and morphological properties of high density polyethylene and polylactide blends | openalex | 2014.0 | 10.1515/polyeng-2013-0174 | https://doi.org/10.1515/polyeng-2013-0174 |
| 31 | Polyethylene and biodegradable mulches for agricultural applications: a review | openalex | 2012.0 | 10.1007/s13593-011-0068-3 | https://doi.org/10.1007/s13593-011-0068-3 |
| 32 | Effect of Blend Ratio of h-LLDPE and LDPE on Tear Properties of Blown Films | crossref | 2012.0 | 10.3139/217.2575 | https://doi.org/10.3139/217.2575 |
| 33 | Properties of LLDPE Film Modified by LDPE | crossref | 2012.0 | 10.1080/03602559.2011.639833 | https://doi.org/10.1080/03602559.2011.639833 |
| 34 | Mechanical and Optical Properies of Poly Lactic Acid Modified Linear- Low Density Polyethylene / Low Density Polyethylene (Lldpe/Ldpe) Blend Blown Film | crossref | 2012.0 | 10.47893/ijmie.2012.1080 | https://doi.org/10.47893/ijmie.2012.1080 |
| 35 | Degradability of linear polyolefins under natural weathering | openalex | 2010.0 | 10.1016/j.polymdegradstab.2010.12.004 | https://doi.org/10.1016/j.polymdegradstab.2010.12.004 |
| 36 | Development of nanofibrous morphology in LDPE/LLDPE/PP blends and its effect on mechanical properties of blend films | crossref | 2008.0 | 10.1002/app.27630 | https://doi.org/10.1002/app.27630 |
| 37 | Investigation of LLDPE/LDPE blown films by response surface methodology | scopus | 2006.0 |  | https://www.scopus.com/inward/record.uri?partnerID=HzOxMe3b&scp=33645302665&origin=inward |
| 38 | Effect of clay on mechanical and gas barrier properties of blown film LDPE/clay nanocomposites | crossref | 2007.0 | 10.1002/app.26839 | https://doi.org/10.1002/app.26839 |
| 39 | APPLICATION OF LDPE/BIODEGRADABLE STARCH BLEND IN BLOWN FILMS | crossref | 2007.0 | 10.1515/polyeng.2007.27.6-7.483 | https://doi.org/10.1515/polyeng.2007.27.6-7.483 |
| 40 | The effect of blending LLDPE comonomers with conventional LDPE on the thermal and mechanical properties of packaging films | scopus | 2005.0 |  | https://www.scopus.com/inward/record.uri?partnerID=HzOxMe3b&scp=33645013988&origin=inward |
| 41 | Correlations between processing parameters, morphology, and properties of blown films of linear low-density polyethylene/low-density polyethylene blends. I. Crystalline biaxial orientation by IR and mechanical properties | scopus | 2006.0 | 10.1002/app.23358 | https://doi.org/10.1002/app.23358 |
| 42 | Properties Predictor for HDPE/LDPE/LLDPE Blends for Shrink Film Applications | crossref | 2006.0 | 10.1177/8756087906062566 | https://doi.org/10.1177/8756087906062566 |
| 43 | Melt Strength, Maximum Output, and Physical Properties of SURPASS TM1 sLLDPE–LDPE Blends in Blown Film | crossref | 2005.0 | 10.1177/8756087905058790 | https://doi.org/10.1177/8756087905058790 |
| 44 | Oriented structure and anisotropy properties of polymer blown films: HDPE, LLDPE and LDPE | crossref | 2004.0 | 10.1016/j.polymer.2003.10.057 | https://doi.org/10.1016/j.polymer.2003.10.057 |
| 45 | Effect of Crystalline Structure on Tear Resistance of LDPE and LLDPE-Blown Films | crossref | 2004.0 | 10.1177/8756087904044753 | https://doi.org/10.1177/8756087904044753 |
| 46 | Microstructure and kinematic aspects of blown film extrusion process: II. Numerical modelling and prediction of LLDPE and LDPE | crossref | 2004.0 | 10.1179/174328904x24871 | https://doi.org/10.1179/174328904x24871 |
| 47 | Morphology and mechanical properties of blown films of a low-density polyethylene/linear low-density polyethylene blend | scopus | 2002.0 | 10.1002/polb.10115 | https://doi.org/10.1002/polb.10115 |
| 48 | The elastic behaviour during capillary extrusion of LDPE/LLDPE blend melts | crossref | 2002.0 | 10.1016/s0142-9418(01)00050-2 | https://doi.org/10.1016/s0142-9418(01)00050-2 |
| 49 | Blending of high-performance LLDPEs with butene-LLDPEs and LDPEs | scopus | 2001.0 | 10.1106/mq49-n4kd-bf0l-64y1 | https://doi.org/10.1106/mq49-n4kd-bf0l-64y1 |
| 50 | BENEFITS OF COEXTRUDED LLDPE/LDPE FILM VS. BLENDED LLDPE/LDPE FILM | crossref | 2000.0 | 10.1177/875608700772677580 | https://doi.org/10.1177/875608700772677580 |
| 51 | Rheology of LLDPE, LDPE and LLDPE/LDPE blends and its relevance to the film blowing process | crossref | 2000.0 | 10.1002/1097-0126(200012)49:12<1580::aid-pi547>3.0.co;2-q | https://doi.org/10.1002/1097-0126(200012)49:12<1580::aid-pi547>3.0.co;2-q |
| 52 | Effect of LLDPE contents on heat seal properties for HDPE/LLDPE blend film HDPE/LLDPEフィルムのヒートシール特性に及ぼすLLDPE添加量の影響 | crossref | 2011.0 | 10.4325/seikeikakou.23.691 | https://doi.org/10.4325/seikeikakou.23.691 |
| 53 | Structural Defects and Processing Limitations for Polymer Film Blowing Applications: A Comprehensive Review of Conventional and Emerging Sustainable Technologies | openalex | 2025.0 | 10.3390/polym17243314 | https://doi.org/10.3390/polym17243314 |
| 54 | Ziegler-Natta Polymerization: HDPE, PP, LLDPE and EPDM | crossref | 2025.0 | 10.31224/4403 | https://doi.org/10.31224/4403 |
| 55 | A perspective on additives for flexible packaging | openalex | 2024.0 | 10.1002/vnl.22135 | https://doi.org/10.1002/vnl.22135 |
| 56 | Overview of the Cast Polyolefin Film Extrusion Technology for Multi-Layer Packaging Applications | openalex | 2023.0 | 10.3390/ma16031071 | https://doi.org/10.3390/ma16031071 |
| 57 | Seal materials in flexible plastic food packaging: A review | openalex | 2023.0 | 10.1002/pts.2732 | https://doi.org/10.1002/pts.2732 |
| 58 | Processing effects on crystal morphology and application performance of blown films from propylene-ethylene random copolymers | openalex | 2024.0 | 10.3144/expresspolymlett.2024.53 | https://doi.org/10.3144/expresspolymlett.2024.53 |
| 59 | The interplay between macromolecular structure, rheology, processing condition, and morphology for (linear) low density polyethylenes in film blowing | openalex | 2023.0 | 10.1016/j.polymer.2023.126566 | https://doi.org/10.1016/j.polymer.2023.126566 |
| 60 | LLDPE matrix with LDPE and UV stabilizer additive to evaluate the interface adhesion impact on the thermal and mechanical degradation | openalex | 2023.0 | 10.1515/eng-2022-0429 | https://doi.org/10.1515/eng-2022-0429 |
| 61 | Silver-titanium polymeric nanocomposite non ecotoxic with bactericide activity | openalex | 2022.0 | 10.1007/s00289-021-04036-7 | https://doi.org/10.1007/s00289-021-04036-7 |
| 62 | Transparent, lightweight, high performance polymer films and their composites | openalex | 2020.0 |  | https://qmro.qmul.ac.uk/xmlui/handle/123456789/68559 |
| 63 | Recycling of low-value packaging films in bitumen blends: A grey-based multi criteria decision making approach considering a set of laboratory performance and environmental impact indicators | openalex | 2021.0 | 10.1016/j.scitotenv.2021.146187 | https://doi.org/10.1016/j.scitotenv.2021.146187 |
| 64 | End-Use Testing of LLDPE Film; Extractables, Solubles, Blocking, and Haze | crossref | 2020.0 | 10.1007/978-1-56990-832-7_7 | https://doi.org/10.1007/978-1-56990-832-7_7 |
| 65 | End-Use Testing of LLDPE Film; Extractables, Solubles, Blocking, and Haze | crossref | 2020.0 | 10.3139/9781569908327.007 | https://doi.org/10.3139/9781569908327.007 |
| 66 | Different Dependence of Tear Strength on Film Orientation of LLDPE Made with Different Co-Monomer | crossref | 2019.0 | 10.3390/polym11030434 | https://doi.org/10.3390/polym11030434 |
| 67 | BP Innovene HDPE/LLDPE process | crossref | 2020.0 | 10.1002/9783527809080.cataz02394 | https://doi.org/10.1002/9783527809080.cataz02394 |
| 68 | Study and Characterization of LLDPE/Polyolefin Elastomer and LLDPE/EPDM Blend: Effect of Chlorinated Water on Blend Performance | crossref | 2018.0 | 10.1016/j.matpr.2018.06.613 | https://doi.org/10.1016/j.matpr.2018.06.613 |
| 69 | Structure–Property–Process Relationship for Blown Films of Bimodal HDPE and Its LLDPE Blend | crossref | 2019.0 | 10.1002/mame.201900325 | https://doi.org/10.1002/mame.201900325 |
| 70 | Influence of Blending Protocol on the Thermal and Mechanical Properties of HDPE/LLDPE Blend-Based Nanocomposites | crossref | 2016.0 | 10.3139/217.3238 | https://doi.org/10.3139/217.3238 |
| 71 | Structural, thermal, and gas transport properties of HDPE/LLDPE blend‐based nanocomposites using a mixture of HDPE‐ g ‐MA and LLDPE‐ g ‐MA as compatibilizer | crossref | 2016.0 | 10.1002/pen.24305 | https://doi.org/10.1002/pen.24305 |
| 72 | Structure evolution during film blowing: An experimental study using in-situ small angle X-ray scattering | openalex | 2015.0 | 10.1016/j.eurpolymj.2015.11.022 | https://doi.org/10.1016/j.eurpolymj.2015.11.022 |
| 73 | The Effect of Graphite Nanoplatelets on the Barrier and Mechanical Properties of LLDPE Films | openalex | 2015.0 |  | https://tigerprints.clemson.edu/all_theses/2290 |
| 74 | Effects of different compatibilizers on the rheological, thermomechanical, and morphological properties of HDPE/LLDPE blend‐based nanocomposites | crossref | 2013.0 | 10.1002/app.39265 | https://doi.org/10.1002/app.39265 |
| 75 | Influence of blending protocol on the thermal and mechanical properties of HDPE/LLDPE blend-based nanocomposites | crossref | 2014.0 | 10.1063/1.4873781 | https://doi.org/10.1063/1.4873781 |
| 76 | Effect of Blending Protocol on the Rheological Properties and Morphology of HDPE/LLDPE Blend-based Nanocomposites | crossref | 2012.0 | 10.3139/217.2567 | https://doi.org/10.3139/217.2567 |
| 77 | Tocopherol stability in controlled release packaging films | openalex | 2009.0 | 10.7282/t3g44qhr | https://doi.org/10.7282/t3g44qhr |
| 78 | Correlation between Structural Parameters and Property of PE Blown Films | openalex | 2005.0 | 10.1177/8756087905059979 | https://doi.org/10.1177/8756087905059979 |
| 79 | High Performance Mineral Reinforcement Concentrate for LLDPE and HMW-HDPE Blown Film Extrusion | crossref | 2002.0 | 10.1106/875608702026263 | https://doi.org/10.1106/875608702026263 |
| 80 | Bridging the Modulus Gap between LLDPE and HDPE | crossref | 2001.0 | 10.1106/d16y-cl3f-gyhd-p9vt | https://doi.org/10.1106/d16y-cl3f-gyhd-p9vt |
| 81 | Optimization studies of blend composition and ageing parameters for making LDPE/HDPE/LLDPE films by response surface methodology | crossref | 2000.0 | 10.1002/1439-2054(20001101)283:1<81::aid-mame81>3.0.co;2-s | https://doi.org/10.1002/1439-2054(20001101)283:1<81::aid-mame81>3.0.co;2-s |
| 82 | Optimization studies of blend composition and ageing parameters for making LDPE/HDPE/LLDPE films by response surface methodology | crossref | 2000.0 | 10.1002/1439-2054(20001101)283:1<81::aid-mame81>3.3.co;2-j | https://doi.org/10.1002/1439-2054(20001101)283:1<81::aid-mame81>3.3.co;2-j |
| 83 | Development of High Barrier Nylon Based Multilayer Films | openalex | 2014.0 |  | https://publications.polymtl.ca/1362/1/2014_MaryamFereydoon.pdf |
| 84 | MODELING THE EFFECTS OF SOLID STATE ORIENTATION ON BLOWN HIGH MOLECULAR WEIGHT HIGH DENSITY POLYETHYLENE FILMS: A COMPOSITE THEORY APPROACH | openalex | 2005.0 |  | http://rave.ohiolink.edu/etdc/view?acc_num=ucin1107958634 |
| 85 | Impact of Microstructural Arrangement of PE-Based Polymers on Electrical Properties: The Case of LLDPE, LDPE and HDPE | crossref | 2025.0 | 10.1109/ceidp61707.2025.11218503 | https://doi.org/10.1109/ceidp61707.2025.11218503 |
| 86 | Development and evaluation of low density polyethylene-based antimicrobial food packaging films containing natural agents | openalex | 2010.0 |  | https://vuir.vu.edu.au/15840/ |
| 87 | Structural and nonlinear J-integral fracture toughness for nanoclay toughened ternary HDPE/LDPE-g-MA/ABS blend nanocomposites | crossref | 2024.0 | 10.1177/00219983241240468 | https://doi.org/10.1177/00219983241240468 |
| 88 | Poly(lactic acid) and Its Blends for Packaging Application: A Review | openalex | 2023.0 | 10.3390/cleantechnol5040066 | https://doi.org/10.3390/cleantechnol5040066 |
| 89 | CRYSTAF, DSC and SAXS Study of the Co-Crystallization, Phase Separation and Lamellar Packing of the Blends with Different Polyethylenes | openalex | 2023.0 | 10.3390/polym15081940 | https://doi.org/10.3390/polym15081940 |
| 90 | Research on Properties of PBAT/CaCO3 Composite Films Modified with Titanate Coupling Agent | openalex | 2023.0 | 10.3390/polym15102379 | https://doi.org/10.3390/polym15102379 |
| 91 | Active Agents Incorporated in Polymeric Substrates to Enhance Antibacterial and Antioxidant Properties in Food Packaging Applications | openalex | 2022.0 | 10.3390/macromol3010001 | https://doi.org/10.3390/macromol3010001 |
| 92 | Biodegradable, UV absorber and thermal stable bioplastic films from waxy corn starch/polyvinyl alcohol blends | openalex | 2023.0 | 10.1007/s13399-022-03683-8 | https://doi.org/10.1007/s13399-022-03683-8 |
| 93 | Effect of the Elongational Flow on the Morphology and Properties of Polymer Systems: A Brief Review | openalex | 2021.0 | 10.3390/polym13203529 | https://doi.org/10.3390/polym13203529 |
| 94 | Progresses in Food Packaging, Food Quality, and Safety—Controlled-Release Antioxidant and/or Antimicrobial Packaging | openalex | 2021.0 | 10.3390/molecules26051263 | https://doi.org/10.3390/molecules26051263 |
| 95 | Morphology, Rheology and Crystallization in Relation to the Viscosity Ratio of Polystyrene/Polypropylene Polymer Blends | openalex | 2020.0 | 10.3390/ma13040926 | https://doi.org/10.3390/ma13040926 |
| 96 | Compatibilization and Characterization of Polylactide and Biopolyethylene Binary Blends by Non-Reactive and Reactive Compatibilization Approaches | openalex | 2020.0 | 10.3390/polym12061344 | https://doi.org/10.3390/polym12061344 |
| 97 | Current trends in biopolymers for food packaging: a review | openalex | 2023.0 | 10.3389/fsufs.2023.1225371 | https://doi.org/10.3389/fsufs.2023.1225371 |
| 98 | Bitumen and Bitumen Modification: A Review on Latest Advances | openalex | 2019.0 | 10.3390/app9040742 | https://doi.org/10.3390/app9040742 |
| 99 | Investigation of physical and rheological properties of LDPE/HDPE/thermoplastic starch biodegradable blend films | crossref | 2022.0 | 10.21203/rs.3.rs-2313459/v1 | https://doi.org/10.21203/rs.3.rs-2313459/v1 |
| 100 | Biodegradable polymers and green-based antimicrobial packaging materials: A mini-review | openalex | 2019.0 | 10.1016/j.aiepr.2019.11.002 | https://doi.org/10.1016/j.aiepr.2019.11.002 |
| 101 | Nanoclays in Food and Beverage Packaging | openalex | 2019.0 | 10.1155/2019/8927167 | https://doi.org/10.1155/2019/8927167 |
| 102 | Thermal and Dynamics Mechanical Analysis of Polypropylene Blown Films with Crude Palm Oil as Plasticizer | openalex | 2019.0 | 10.22146/ijc.30460 | https://doi.org/10.22146/ijc.30460 |
| 103 | Crystal Structure Evolution of UHMWPE/HDPE Blend Fibers Prepared by Melt Spinning | openalex | 2017.0 | 10.3390/polym9030096 | https://doi.org/10.3390/polym9030096 |
| 104 | Investigation of mechanical, thermal and recycled characteristics of reinforced ternary blends of LDPE/LLDPE/HDPE by ANOVA | crossref | 2018.0 | 10.1088/2053-1591/aac792 | https://doi.org/10.1088/2053-1591/aac792 |
| 105 | Durability of nanosized oxygen-barrier coatings on polymers | openalex | 2002.0 | 10.1016/s0079-6425(02)00002-6 | https://doi.org/10.1016/s0079-6425(02)00002-6 |
| 106 | Puncture Impact Behavior of Glass Plate Fitted With a Polymeric Film | crossref | 2021.0 | 10.1115/1.0004104v | https://doi.org/10.1115/1.0004104v |
| 107 | Rheological and thermal properties of m-LLDPE blends with m-HDPE and LDPE | crossref | 2002.0 | 10.1016/s0032-3861(02)00201-x | https://doi.org/10.1016/s0032-3861(02)00201-x |
| 108 | Hardware for Blown Film | crossref | 2019.0 | 10.1007/978-1-56990-697-2_4 | https://doi.org/10.1007/978-1-56990-697-2_4 |
| 109 | Materials for Blown Film | crossref | 2019.0 | 10.1007/978-1-56990-697-2_1 | https://doi.org/10.1007/978-1-56990-697-2_1 |
| 110 | Materials for Blown Film | crossref | 2018.0 | 10.3139/9781569906972.001 | https://doi.org/10.3139/9781569906972.001 |
| 111 | PP-CBW/m-LLDPE/micro-CaCO 3 composite films manufactured from bumper waste by blown film extrusion | crossref | 2019.0 | 10.1051/matecconf/201928103001 | https://doi.org/10.1051/matecconf/201928103001 |
| 112 | Analysis of dart impact resistance of low-density polyethylene and linear low-density polyethylene blown films via an improved instrumented impact test method | crossref | 2012.0 | 10.1177/8756087911434184 | https://doi.org/10.1177/8756087911434184 |
| 113 | Impact of branching on the UV degradation of metallocene LLDPE | crossref | 2011.0 | 10.1007/s10965-010-9561-7 | https://doi.org/10.1007/s10965-010-9561-7 |
| 114 | Hardware for Blown Film | crossref | 2011.0 | 10.3139/9783446428195.003 | https://doi.org/10.3139/9783446428195.003 |
| 115 | Blown Film Extrusion | crossref | 2011.0 | 10.3139/9783446428195.fm | https://doi.org/10.3139/9783446428195.fm |
| 116 | The Influence of Solid-State Morphology on the Dart Impact Strength of Linear Low-Density Polyethylene Blown Films | crossref | 2005.0 | 10.1177/8756087905054148 | https://doi.org/10.1177/8756087905054148 |
| 117 | Metallocene LLDPE Films for Heavy-Duty Sack Applications | crossref | 2004.0 | 10.1177/8756087904047212 | https://doi.org/10.1177/8756087904047212 |
| 118 | Polymer processing aids eliminate melt fracture in LLDPE blown film | crossref | 2002.0 | 10.1016/s1464-391x(02)80024-1 | https://doi.org/10.1016/s1464-391x(02)80024-1 |
| 119 | Blown Film Characterization of Binary Blends of Metallocene-Catalyzed LLDPES | crossref | 2001.0 | 10.1106/2tuc-fv80-furu-qxwb | https://doi.org/10.1106/2tuc-fv80-furu-qxwb |
| 120 | Melt Miscibility and Mechanical Properties of Metallocene LLDPE blends with HDPE: Influence of Mw of LLDPE | crossref | 2006.0 | 10.1295/polymj.pj2005254 | https://doi.org/10.1295/polymj.pj2005254 |
| 121 | Blown Film Characterization of Binary Blends of Metallocene-catalyzed LLDPES | crossref | 2001.0 | 10.1177/875608701772677732 | https://doi.org/10.1177/875608701772677732 |
| 122 | Crystallization Studies of LLDPE during Tubular Blown Film Processing | crossref | 2001.0 | 10.3139/217.1624 | https://doi.org/10.3139/217.1624 |
| 123 | TRADE-OFFS IN BLOWN FILM LLDPE TYPE RESINS FROM CHROMIUM, METALLOCENE AND ZIEGLER-NATTA CATALYSTS | crossref | 2000.0 | 10.1106/ypu9-cjw7-acqy-walp | https://doi.org/10.1106/ypu9-cjw7-acqy-walp |
| 124 | Simplified Model and Approach to Transform Infrared Surface Temperature to Film Effectiveness in a Conjugate Heat Transfer Experiment | crossref | 2025.0 | 10.1115/gt2025-153214 | https://doi.org/10.1115/gt2025-153214 |
| 125 | High-temperature and High-speed Air Film Floating Ring Seal Constant Clearance Design and Leakage Analysis | crossref | 2026.0 | 10.3901/jme.260420 | https://doi.org/10.3901/jme.260420 |
| 126 | Effect of Antioxidants and Compatibilizers on Gel Formation and Film Quality of Polyethylene Films With Recycled Content | openalex | 2026.0 | 10.1002/pts.70106 | https://doi.org/10.1002/pts.70106 |
| 127 | A New Test Facility for Investigating Leaf-Seal Cavity Ingestion at Combustor-Turbine Interface | crossref | 2025.0 | 10.1115/gt2025-152927 | https://doi.org/10.1115/gt2025-152927 |
| 128 | Mass-Heat Coupling in Film Cooling Experiments — The Influence of Temperature and Turbulence on the Dufour Effect | crossref | 2023.0 | 10.1115/gt2023-101638 | https://doi.org/10.1115/gt2023-101638 |
| 129 | Brush Seal Wear Measurements for High-Speed, High-Temperature, Low-Pressure-Turbine Applications | crossref | 2023.0 | 10.1115/gt2023-103022 | https://doi.org/10.1115/gt2023-103022 |
| 130 | Evaluating Effectiveness of Multi-Component Waste Plastic Bags on Bitumen Properties: Physical, Rheological, and Aging | openalex | 2024.0 | 10.3390/polym16121669 | https://doi.org/10.3390/polym16121669 |
| 131 | Steady-State Characteristics of Spiral Groove Floating Ring Gas-film Seal Considering Temperature-Viscosity Effect | crossref | 2023.0 | 10.47176/jafm.16.04.1432 | https://doi.org/10.47176/jafm.16.04.1432 |
| 132 | HEAT TRANSFER ANALYSIS ON PLATINUM-BASED THIN-FILM TEMPERATURE SENSOR ELEMENT FOR LIQUID TEMPERATURE MEASUREMENT APPLICATIONS | crossref | 2021.0 | 10.1615/heattransres.2021037906 | https://doi.org/10.1615/heattransres.2021037906 |
| 133 | Evaluation and optimization of seal behaviour through solid contamination of heat‐sealed films | openalex | 2019.0 | 10.1002/pts.2442 | https://doi.org/10.1002/pts.2442 |
| 134 | High Temperature Brush Seal Development | crossref | 2017.0 | 10.1115/gt2017-63091 | https://doi.org/10.1115/gt2017-63091 |
| 135 | FILM BOILING COLLAPSE TEMPERATURE AND BOILING HEAT TRANSFER CORRELATIONS THROUGH TWO-DIMENSIONAL TEMPERATURE FIELD MEASUREMENT AND OBSERVATION OF LIQUID-SOLID CONTACT | crossref | 2018.0 | 10.1615/ihtc16.bae.023658 | https://doi.org/10.1615/ihtc16.bae.023658 |
| 136 | Theoretical analysis and experiment on gas film temperature in a spiral groove dry gas seal under high speed and pressure | crossref | 2016.0 | 10.1016/j.ijheatmasstransfer.2016.01.045 | https://doi.org/10.1016/j.ijheatmasstransfer.2016.01.045 |
| 137 | Failure analysis of LLDPE based materials | openalex | 2018.0 |  | http://hdl.handle.net/10019.1/103525 |
| 138 | Initiation of Combustion of Coal Particles Coated with a Water Film in a High-Temperature Air Flow | crossref | 2016.0 | 10.15372/fgv20160506 | https://doi.org/10.15372/fgv20160506 |
| 139 | Boiling Heat Transfer Characteristics and Film Boiling Collapse Temperature through the Two-Dimensional Temperature Field Measurement | crossref | 2014.0 | 10.1615/ihtc15.pbl.009511 | https://doi.org/10.1615/ihtc15.pbl.009511 |
| 140 | Calculation Of Young Modulus Of Polyolefin Nanocomposites By Halpin Tsai Model | openalex | 2011.0 |  | http://hdl.handle.net/11527/5654 |
| 141 | Velocity and Temperature Fields on Laminar Forced Film Condensation of Pure Vapour | crossref | 2010.0 | 10.1007/978-3-642-12581-2_10 | https://doi.org/10.1007/978-3-642-12581-2_10 |
| 142 | Heat Seal Strength of Barrier Films Used in Vacuum Insulation Panels At Room Temperature and At -130°C | crossref | 2008.0 | 10.1177/8756087908089092 | https://doi.org/10.1177/8756087908089092 |
| 143 | Fourier-transform rheology applied on homopolymer melts of different architectures-Experiments and simulations | openalex | 2008.0 | 10.26083/tuprints-00000768 | https://doi.org/10.26083/tuprints-00000768 |
| 144 | Use of the Adiabatic Wall Temperature in Film Cooling to Predict Wall Heat Flux and Temperature | crossref | 2008.0 | 10.1115/gt2008-51424 | https://doi.org/10.1115/gt2008-51424 |
| 145 | Plastomer-mVLDPE Blends for High Performance Heat Sealing Applications | scopus | 2003.0 |  | https://www.scopus.com/inward/record.uri?partnerID=HzOxMe3b&scp=1142265475&origin=inward |
| 146 | Thermorheology and processing of polyethylene blends : macromolecular structure effects | openalex | 2008.0 | 10.14288/1.0058564 | https://doi.org/10.14288/1.0058564 |
| 147 | Metallocene-Catalyzed Linear Low Density Polyethylene - mLLDPE | crossref | 2004.0 | 10.1016/b978-1-884207-94-5.50031-3 | https://doi.org/10.1016/b978-1-884207-94-5.50031-3 |
| 148 | Physical and optical properties of sol-gel nano-silver doped silica film on glass substrate as a function of heat-treatment temperature | crossref | 2003.0 | 10.1063/1.1571215 | https://doi.org/10.1063/1.1571215 |
| 149 | Heat seal coating and coated film | crossref | 2002.0 | 10.1016/s1350-4789(02)08026-1 | https://doi.org/10.1016/s1350-4789(02)08026-1 |
| 150 | Fourier-transform rheology applied on homopolymer melts of different architectures - experiments and finite element simulations | openalex | 2006.0 |  | http://hdl.handle.net/11858/00-001M-0000-000F-80BF-B |
| 151 | Predicting the Heat Seal Performance of Ionomer Films | crossref | 2002.0 | 10.1177/8756087902018003002 | https://doi.org/10.1177/8756087902018003002 |
| 152 | Heat Transfer from a Local Heat Source to Subcooled Liquid Film | crossref | 2001.0 | 10.1023/a:1012381010962 | https://doi.org/10.1023/a:1012381010962 |
| 153 | Recycling of Poly(Propylene) Based Car Bumpers in the Perspective of Polyolefin Nanoclay Composite Film Production | openalex | 2025.0 | 10.3390/recycling10030095 | https://doi.org/10.3390/recycling10030095 |
| 154 | Industrial Synthesis of Linear Low‐Density Polyethylene with H‐Shape Long‐Chain‐Branching Structures Using Ziegler‐Natta Catalysts | openalex | 2024.0 | 10.1002/mren.202400044 | https://doi.org/10.1002/mren.202400044 |
| 155 | Polymers and rheology: A tale of give and take | openalex | 2023.0 | 10.1016/j.polymer.2023.125811 | https://doi.org/10.1016/j.polymer.2023.125811 |
| 156 | Tuning dielectric response of polyethylene by low gamma dose: Molecular mobility study improvement by dipolar probes implementation | openalex | 2023.0 | 10.1016/j.jnoncrysol.2023.122606 | https://doi.org/10.1016/j.jnoncrysol.2023.122606 |
| 157 | Expanding plastics recycling technologies: chemical aspects, technology status and challenges | openalex | 2022.0 | 10.1039/d2gc02588d | https://doi.org/10.1039/d2gc02588d |
| 158 | Abiotic aging assisted bio-oxidation and degradation of LLDPE/LDPE packaging polyethylene film by stimulated enrichment culture | crossref | 2022.0 | 10.1016/j.polymdegradstab.2022.110156 | https://doi.org/10.1016/j.polymdegradstab.2022.110156 |
| 159 | Shear and Extensional Rheology of Linear and Branched Polybutylene Succinate Blends | openalex | 2021.0 | 10.3390/polym13040652 | https://doi.org/10.3390/polym13040652 |
| 160 | Blown film cooling numerical and experimental investigations | crossref | 2024.0 | 10.5772/intechopen.1002412 | https://doi.org/10.5772/intechopen.1002412 |
| 161 | Direct Synthesis of Polar-Functionalized Linear Low-Density Polyethylene (LLDPE) and Low-Density Polyethylene (LDPE) | crossref |  | 10.1021/acs.macromol.8b00467.s003 | https://doi.org/10.1021/acs.macromol.8b00467.s003 |
| 162 | Direct Synthesis of Polar-Functionalized Linear Low-Density Polyethylene (LLDPE) and Low-Density Polyethylene (LDPE) | crossref |  | 10.1021/acs.macromol.8b00467.s004 | https://doi.org/10.1021/acs.macromol.8b00467.s004 |
| 163 | Direct Synthesis of Polar-Functionalized Linear Low-Density Polyethylene (LLDPE) and Low-Density Polyethylene (LDPE) | crossref |  | 10.1021/acs.macromol.8b00467.s001 | https://doi.org/10.1021/acs.macromol.8b00467.s001 |
| 164 | Direct Synthesis of Polar-Functionalized Linear Low-Density Polyethylene (LLDPE) and Low-Density Polyethylene (LDPE) | crossref |  | 10.1021/acs.macromol.8b00467.s005 | https://doi.org/10.1021/acs.macromol.8b00467.s005 |
| 165 | Direct Synthesis of Polar-Functionalized Linear Low-Density Polyethylene (LLDPE) and Low-Density Polyethylene (LDPE) | crossref |  | 10.1021/acs.macromol.8b00467.s002 | https://doi.org/10.1021/acs.macromol.8b00467.s002 |
| 166 | Implications of melt compatibility/incompatibility on thermal and mechanical properties of metallocene and Ziegler–Natta linear low density polyethylene (LLDPE) blends with high density polyethylene (HDPE): influence of composition distribution and branch content of LLDPE | crossref | 2004.0 | 10.1002/pi.1528 | https://doi.org/10.1002/pi.1528 |
| 167 | Review for "Model-Based Optimization of Properties of Post-Consumer Recycled PP/PE Blends via Compatibilization" | crossref | 2025.0 | 10.1039/d5lp00321k/v1/review1 | https://doi.org/10.1039/d5lp00321k/v1/review1 |
| 168 | Investigation of The Effects of Using Recycled Raw Materials on The Mechanical Properties of Pe Film Produced by Blown Film Extrusion Technology | crossref | 2024.0 | 10.56038/oprd.v5i1.501 | https://doi.org/10.56038/oprd.v5i1.501 |
| 169 | A Review of Weathering Studies in Plastics and Biocomposites—Effects on Mechanical Properties and Emissions of Volatile Organic Compounds (VOCs) | openalex | 2024.0 | 10.3390/polym16081103 | https://doi.org/10.3390/polym16081103 |
| 170 | Biodegradable blown film composite from poly (butylene adipate-co-terephthalate) and talc: Effect of uniaxial stretching on mechanical and barrier properties | openalex | 2023.0 | 10.1016/j.fpsl.2023.101147 | https://doi.org/10.1016/j.fpsl.2023.101147 |
| 171 | Manufacturing and Properties of Recycled Polyethylene Films with an Inorganic Filler by the Extrusion Blow Moulding Method | openalex | 2019.0 | 10.1007/978-3-030-16943-5_54 | https://doi.org/10.1007/978-3-030-16943-5_54 |
| 172 | Studies On Compatibilization Of Recycled Polyethylene/Thermoplastic Starch Blends By Using Different Compatibilizer | openalex | 2019.0 | 10.1515/chem-2019-0064 | https://doi.org/10.1515/chem-2019-0064 |
| 173 | Blending of Low-Density Polyethylene and Poly(Butylene Succinate) (LDPE/PBS) with Polyethylene–Graft–Maleic Anhydride (PE–g–MA) as a Compatibilizer on the Phase Morphology, Mechanical and Thermal Properties | openalex | 2023.0 | 10.3390/polym15020261 | https://doi.org/10.3390/polym15020261 |
| 174 | Tailoring PLA/ABS Blends Compatibilized with SEBS-g-MA through Annealing Heat Treatment | openalex | 2023.0 | 10.3390/polym15163434 | https://doi.org/10.3390/polym15163434 |
| 175 | Effect of compatibilizers on polyethylene‐eucalyptus lignin blends | openalex | 2023.0 | 10.1002/app.53695 | https://doi.org/10.1002/app.53695 |
| 176 | A facile evaluation on melt crystallization kinetics and thermal properties of low-density polyethylene (LDPE)/Recycled polyethylene terephthalate (RPET) blends | openalex | 2019.0 | 10.1016/j.aiepr.2019.05.002 | https://doi.org/10.1016/j.aiepr.2019.05.002 |
| 177 | Meltblown technology for production of polymeric microfibers/nanofibers: A review | openalex | 2019.0 | 10.1063/1.5116336 | https://doi.org/10.1063/1.5116336 |
| 178 | INVESTIGATION OF LLDPE/LDPE BLOWN FILMS BY RESPONSE SURFACE METHODOLOGY | openalex | 2006.0 |  | https://www.sid.ir/en/VEWSSID/J_pdf/81320060207.pdf |
| 179 | Melt strength of polypropylene: Its relevance to thermoforming | openalex | 1998.0 | 10.1002/pen.10362 | https://doi.org/10.1002/pen.10362 |
| 180 | Advancements in Biodegradable Active Films for Food Packaging: Effects of Nano/Microcapsule Incorporation | openalex | 2022.0 | 10.3390/foods11050760 | https://doi.org/10.3390/foods11050760 |
| 181 | Active Flexible Films for Food Packaging: A Review | openalex | 2022.0 | 10.3390/polym14122442 | https://doi.org/10.3390/polym14122442 |
| 182 | Mosquito‐repellent controlled‐release formulations for fighting infectious diseases | openalex | 2021.0 | 10.1186/s12936-021-03681-7 | https://doi.org/10.1186/s12936-021-03681-7 |
| 183 | Multiphysics modelling of manufacturing processes: A review | openalex | 2018.0 | 10.1177/1687814018766188 | https://doi.org/10.1177/1687814018766188 |
| 184 | Process monitoring and visualization solutions for hot-melt extrusion: a review | openalex | 2013.0 | 10.1111/jphp.12123 | https://doi.org/10.1111/jphp.12123 |
| 185 | Spherilene Process LLDPE for Conventionally Blown Shrink Film | crossref | 1998.0 | 10.1016/b978-188420759-4.50039-5 | https://doi.org/10.1016/b978-188420759-4.50039-5 |
| 186 | Processing of lldpe blown film | crossref | 1988.0 | 10.1016/0306-3747(88)90465-4 | https://doi.org/10.1016/0306-3747(88)90465-4 |
| 187 | Influence of compatibilizer on morphology and mechanical properties of LLDPE/NR blends produced by blown film and chill roll cast film extrusion | crossref |  | 10.58837/chula.the.1999.1454 | https://doi.org/10.58837/chula.the.1999.1454 |
| 188 | 吹膜工艺用LLDPE 7042树脂 - chemategroup.com | duckduckgo |  |  | https://www.chemategroup.com/zh-CN/lldpe-7042/ |
| 189 | A study of mechanical properties and processability of blown films using b-LLDPE and LDPE blends | openalex | 2010.0 |  | http://eprints.kfupm.edu.sa/136335/1/Complete_Thesis.pdf |
| 190 | Trade-offs in Blown Film Processing-Structure-Property Behavior of LLDPE Type Resins from Chromium, Metallocene and Ziegler-Natta Catalysts | crossref | 1999.0 | 10.1016/b978-188420776-1.50019-3 | https://doi.org/10.1016/b978-188420776-1.50019-3 |
| 191 | Blown Film Characterization of Metallocene Resins Made in the Phillips Slurry Loop Process | crossref | 1998.0 | 10.1016/b978-188420759-4.50040-1 | https://doi.org/10.1016/b978-188420759-4.50040-1 |
| 192 | 你的吹膜难题解决了吗？茂金属优异性能了解一下 _塑料资讯_塑料行业新闻-搜料¦工程塑料超市 | duckduckgo |  |  | https://www.soliao.com/news/qita/48524.html |
| 193 | 茂金属聚乙烯和线性聚乙烯的区别 - 塑问 | duckduckgo |  |  | https://www.suwen8.com/web/view/sw/headline/ArticleAction-article_detail.action?articleId=8a2a22736b9bd57e016bb04795c500d5 |
| 194 | 茂金属聚乙烯薄膜：高功能包装首选_塑料资讯_塑料行业新闻-搜料¦工程塑料超市 | duckduckgo |  |  | https://www.soliao.com/news/zhidao/884.html |
| 195 | Functionalization of LDPE and mLLDPE via grafting trans-ethylene-1,2-dicarboxylic acid by reactive extrusion | openalex | 2010.0 | 10.3144/expresspolymlett.2010.21 | https://doi.org/10.3144/expresspolymlett.2010.21 |
| 196 | A Journey from Processing to Recycling of Multilayer Waste Films: A Review of Main Challenges and Prospects | openalex | 2022.0 | 10.3390/polym14122319 | https://doi.org/10.3390/polym14122319 |
| 197 | 低密度聚乙烯2426H吹膜工艺研究 ¦ PDF - Scribd | duckduckgo |  |  | https://www.scribd.com/document/884229286/低密度聚乙烯2426H吹膜工艺研究 |
| 198 | 低密度聚乙烯2426H吹膜工艺研究-技术综述-技术-广州江外江信息科技有... | duckduckgo |  |  | https://www.ip1689.com/jishu/show.php?itemid=680 |
| 199 | LDPE(低密度聚乙烯) 2426H/中海壳牌 - santplas.com | duckduckgo |  |  | https://www.santplas.com/uploads/soft/20230810/1-230Q01Q311J5.PDF |
| 200 | Review of recycling waste plastics in asphalt paving materials | openalex | 2022.0 | 10.1016/j.jtte.2022.07.002 | https://doi.org/10.1016/j.jtte.2022.07.002 |
| 201 | Recycling of polyamides: Processes and conditions | openalex | 2023.0 | 10.1002/pol.20230154 | https://doi.org/10.1002/pol.20230154 |
| 202 | Thermo-Mechanical Recycling Via Ultrahigh-Speed Extrusion of Film-Grade Recycled Ldpe and Injection Molding | crossref | 2023.0 | 10.2139/ssrn.4429376 | https://doi.org/10.2139/ssrn.4429376 |
| 203 | Thermo-Mechanical Recycling Via Ultrahigh-Speed Extrusion of Film-Grade Recycled Ldpe and Injection Molding | crossref | 2023.0 | 10.2139/ssrn.4498144 | https://doi.org/10.2139/ssrn.4498144 |
| 204 | Thermal, morphological and mechanical properties of recycled Al film label /LLDPE composites | crossref | 2026.0 | 10.22299/apst.2026.282047 | https://doi.org/10.22299/apst.2026.282047 |
| 205 | Kompozyty PET i ich zastosowanie w obliczu wyzwań zielonej chemii – przegląd literaturowy | openalex | 2025.0 | 10.14314/polimery.2025.4.1 | https://doi.org/10.14314/polimery.2025.4.1 |
| 206 | Technical, Economic, and Environmental Comparison of Closed-Loop Recycling Technologies for Common Plastics | openalex | 2023.0 | 10.1021/acssuschemeng.2c05497 | https://doi.org/10.1021/acssuschemeng.2c05497 |
| 207 | Managing Plastic Waste─Sorting, Recycling, Disposal, and Product Redesign | openalex | 2021.0 | 10.1021/acssuschemeng.1c05013 | https://doi.org/10.1021/acssuschemeng.1c05013 |
| 208 | Recycling of multi-material multilayer plastic packaging: Current trends and future scenarios | openalex | 2021.0 | 10.1016/j.resconrec.2021.105905 | https://doi.org/10.1016/j.resconrec.2021.105905 |
| 209 | CN223131133U - 一种吹膜机边角料回收装置 - Google Patents | duckduckgo |  |  | https://patents.google.com/patent/CN223131133U/zh |
| 210 | 如何高效回收吹塑薄膜边角料？ - shuliyrecycle.com | duckduckgo |  |  | https://www.shuliyrecycle.com/zh/how-to-recycle-blow-molded-film-scraps/ |
| 211 | 一种吹膜机边角料回收装置的制作方法 - X技术网 | duckduckgo |  |  | https://www.xjishu.com/zhuanli/35/202421890723.html |
| 212 | Improved thermal conductivity of immiscible polyamide 6 (PA6)/polyolefin elastomer (POE) blend by controlling selective localization of aluminum nitride (AlN) | crossref | 2025.0 | 10.1007/s13726-024-01352-3 | https://doi.org/10.1007/s13726-024-01352-3 |
| 213 | Understanding the factors affecting the seal integrity in heat sealed flexible food packages: A review | openalex | 2021.0 | 10.1002/pts.2564 | https://doi.org/10.1002/pts.2564 |
| 214 | Radial seal ring for a puncture device | crossref | 2010.0 | 10.1016/s1350-4789(10)70555-9 | https://doi.org/10.1016/s1350-4789(10)70555-9 |
| 215 | Puncture seal | crossref | 2008.0 | 10.1016/s1350-4789(08)70487-2 | https://doi.org/10.1016/s1350-4789(08)70487-2 |
| 216 | Ultra Low Density Polyethylene - ULDPE | crossref | 2004.0 | 10.1016/b978-1-884207-94-5.50028-3 | https://doi.org/10.1016/b978-1-884207-94-5.50028-3 |
| 217 | A Systematic Investigation on the Influence of Intumescent Flame Retardants on the Properties of Ethylene Vinyl Acetate (EVA)/Liner Low Density Polyethylene (LLDPE) Blends | crossref | 2023.0 | 10.3390/molecules28031023 | https://doi.org/10.3390/molecules28031023 |
| 218 | 2026春季柔韧EVA吹膜料厂家直供｜支持定制VA含量与小批量试样 | duckduckgo |  |  | https://www.1688.com/wiki/zh/eva/WKff94jkdfnoqo |
| 219 | EVA 的 VA 含量对性能有什么影响 - b2bwiki.baidu.com | duckduckgo |  |  | https://b2bwiki.baidu.com/article/d23d74o3638oc843s8f0 |
| 220 | EVA 乙烯 – 醋酸乙烯共聚物塑胶原料，按 VA 含量分为发泡、注塑、吹膜... | duckduckgo |  |  | https://www.zaotop.com/?product=eva-乙烯-醋酸乙烯共聚物塑胶原料，按-va-含量分为发泡 |
| 221 | Non-isothermal crystallization kinetics behavior of ethylene-methyl acrylate copolymer and ethylene-methyl acrylate copolymer/chloroprene rubber thermoplastic vulcanizate | crossref | 2024.0 | 10.1080/00222348.2024.2301852 | https://doi.org/10.1080/00222348.2024.2301852 |
| 222 | Thin films as an emerging platform for drug delivery | openalex | 2016.0 | 10.1016/j.ajps.2016.05.004 | https://doi.org/10.1016/j.ajps.2016.05.004 |
| 223 | Rapid ordering of block copolymer thin films | openalex | 2016.0 | 10.1088/0953-8984/28/40/403002 | https://doi.org/10.1088/0953-8984/28/40/403002 |
| 224 | EMA共聚物 ¦ 埃克森美孚化工 - exxonmobilchemical.com.cn | duckduckgo |  |  | https://www.exxonmobilchemical.com.cn/zh-cn/resources/product-data-sheets/polyethylene/ema-copolymers |
| 225 | 乙烯-丙烯酸甲酯共聚物（EMA）基础知识分享 - 知乎 | duckduckgo |  |  | https://zhuanlan.zhihu.com/p/586215093 |
| 226 | EMA (乙烯-丙烯酸甲酯共聚物)介绍以及应用领域 | duckduckgo |  |  | https://www.yjbtzsujiao.com/page61?article_id=129&_l=zh_CN |
| 227 | Comparative Studies on Cow Horn Powder and Calcium Carbonate Filled High-Density Polyethylene Composites: An Evaluation of Mechanical and Physical Properties | crossref | 2026.0 | 10.55248/gengpi.07.0526.c1138 | https://doi.org/10.55248/gengpi.07.0526.c1138 |
| 228 | Starch consolidation of calcium carbonate as a tool to develop lightweight fillers for LDPE-based plastics | openalex | 2022.0 | 10.1016/j.ijbiomac.2022.11.219 | https://doi.org/10.1016/j.ijbiomac.2022.11.219 |
| 229 | Film Blowing of Biodegradable Polymer Nanocomposites for Agricultural Applications | openalex | 2021.0 | 10.1002/mame.202100177 | https://doi.org/10.1002/mame.202100177 |
| 230 | Sustainable Multiscale High-Haze Transparent Cellulose Fiber Film via a Biomimetic Approach | crossref |  | 10.1021/acsmaterialslett.1c00630.s001 | https://doi.org/10.1021/acsmaterialslett.1c00630.s001 |
| 231 | Sustainable Multiscale High-Haze Transparent Cellulose Fiber Film via a Biomimetic Approach | crossref |  | 10.1021/acsmaterialslett.1c00630.s003 | https://doi.org/10.1021/acsmaterialslett.1c00630.s003 |
| 232 | Sustainable Multiscale High-Haze Transparent Cellulose Fiber Film via a Biomimetic Approach | crossref |  | 10.1021/acsmaterialslett.1c00630.s002 | https://doi.org/10.1021/acsmaterialslett.1c00630.s002 |
| 233 | Facile and Large-Area Preparation of Polypyrrole Film for Low-Haze Transparent Supercapacitors | crossref |  | 10.1021/acsami.8b13503.s001 | https://doi.org/10.1021/acsami.8b13503.s001 |
| 234 | 硫酸钡填充食品级母粒PE吹膜农膜地膜塑胶袋吹塑高透明母料食品级-淘宝... | duckduckgo |  |  | https://www.taobao.com/list/item/SjNuY3k2SWc5M2VRbzhGMFBxeHZYdz09.htm |
| 235 | 2026高透明硫酸钡填充母料（透光率≥90%）¦ 适用于PP/PE薄膜 ¦ 1688B2B... | duckduckgo |  |  | https://www.1688.com/wiki/zh/filler-masterbatch/WKfii27mlhotfk |
| 236 | 纳米透明硫酸钡母粒现状和发展分析 (优.选)_百度文库 | duckduckgo |  |  | https://wenku.baidu.com/view/08e07a62e618964bcf84b9d528ea81c758f52e60.html |
| 237 | Flow Instability in LLDPE Processing and Its Control by Fluoropolymer Additives * | crossref | 2020.0 | 10.1201/9780367813734-24 | https://doi.org/10.1201/9780367813734-24 |
| 238 | Dielectric response of LLDPE/Clay nanocomposite melt compounded from a masterbatch | crossref | 2012.0 | 10.1109/elinsl.2012.6251550 | https://doi.org/10.1109/elinsl.2012.6251550 |
| 239 | The role of surface energy of boron nitride on gross melt fracture elimination of polymers | openalex | 2011.0 | 10.14288/1.0089232 | https://doi.org/10.14288/1.0089232 |
| 240 | Ppa母粒 - 功能母粒 - 山东北宏新材料科技有限公司 | duckduckgo |  |  | https://www.xinbeihong.com/index/Article/show/cat_id/8/id/11 |
| 241 | 聚乙烯加工助剂（Ppa）母粒¦ PPA母粒 - zh.dcmasterbatch.com | duckduckgo |  |  | https://zh.dcmasterbatch.com/products/pe-functional-masterbatch/polyethylene-processing-aid--ppa--masterbatch |
| 242 | Ppa母粒（流变母粒、流平母粒） （Wf-sf120） | duckduckgo |  |  | http://www.welfield.com.cn/pro_view-16.html |
| 243 | Mechanical Recycling of Packaging Plastics: A Review | openalex | 2020.0 | 10.1002/marc.202000415 | https://doi.org/10.1002/marc.202000415 |
| 244 | Influence of compatibilizer on the properties of low-density polyethylene/polyamide 6 blends obtained by mechanical recycling of multilayer film waste | openalex | 2018.0 | 10.1177/0734242x18777795 | https://doi.org/10.1177/0734242x18777795 |
| 245 | Recycling of Polymer-Based Multilayer Packaging: A Review | openalex | 2017.0 | 10.3390/recycling3010001 | https://doi.org/10.3390/recycling3010001 |
| 246 | Use of maleic anhydride grafted recycled polyethylene treated by irradiation in bitumen modification | crossref | 2016.0 | 10.14311/ee.2016.155 | https://doi.org/10.14311/ee.2016.155 |
| 247 | 马来酸酐接枝相容剂 - 百度百科 | duckduckgo |  |  | https://baike.baidu.com/item/马来酸酐接枝相容剂/9303471 |
| 248 | 马来酸酐接枝PE相容剂到底有多神奇？一文看懂增韧改性黑科技 | duckduckgo |  |  | https://bk.taobao.com/k/zengsuji_12363/e81d9b9d5b11a107aa787bab2d883b25.html |
| 249 | 马来酸酐接枝聚乙烯 - 百度百科 | duckduckgo |  |  | https://baike.baidu.com/item/马来酸酐接枝聚乙烯/244100 |
| 250 | RESEARCH PROGRESS ON BIOFILM CARRIER MATERIALS IN AQUACULTURE WASTEWATER TREATMENT | openalex | 2026.0 | 10.3724/1000-3207.2026.2025.0422 | https://doi.org/10.3724/1000-3207.2026.2025.0422 |
| 251 | A review of mechanical abuse safety of lithium-ion batteries under different aging approaches | openalex | 2025.0 | 10.1360/sst-2024-0317 | https://doi.org/10.1360/sst-2024-0317 |
| 252 | QUANTIFICATION OF A VITAL NUCLEATING AGENT FOR IMPROVING THE RECOVERY RATE OF RECYCLED ETHYLENE-PROPYLENE IMPACT COPOLYMER PLASTICS USING VIBRATIONAL SPECTROSCOPY AND MULTIVARIATE ANALYSIS | openalex | 2023.0 | 10.35741/issn.0258-2724.58.5.40 | https://doi.org/10.35741/issn.0258-2724.58.5.40 |
| 253 | The Latest Research of Osmotic Dehydration on Osmotic Agents | crossref | 2022.0 | 10.12677/hjfns.2022.112023 | https://doi.org/10.12677/hjfns.2022.112023 |
| 254 | 塑料透明剂_百度百科 | duckduckgo |  |  | https://baike.baidu.com/item/塑料透明剂/958035 |
| 255 | 全面解读各类成核剂的作用机理及效用! - 知乎 | duckduckgo |  |  | https://zhuanlan.zhihu.com/p/6196491604 |
| 256 | 成核剂 ¦ 提升结晶性能与透明度 ¦ 洛特化工 | duckduckgo |  |  | https://www.jxlotchem.com/nucleating-agent/ |
| 257 | Printability and Mechanical Properties of Polyethylene and Polyethylene/Nylon Blend Parts Made by Selective Laser Sintering | crossref | 2022.0 | 10.2172/1887106 | https://doi.org/10.2172/1887106 |
| 258 | Melt-Electrospun Polyethylene Nanofiber Obtained from Polyethylene/Polyvinyl Butyral Blend Film | crossref | 2020.0 | 10.3390/polym12020457 | https://doi.org/10.3390/polym12020457 |
| 259 | Characterization of Chitosan and Polyethylene glycol Blend Film | crossref | 2019.0 | 10.21608/ejchem.2019.11668.1743 | https://doi.org/10.21608/ejchem.2019.11668.1743 |
| 260 | Nature：抗氧化剂可能促进癌细胞的扩散 | crossref | 2015.0 | 10.14218/mrp.2015.060 | https://doi.org/10.14218/mrp.2015.060 |
| 261 | 巴斯夫扩链剂Joncryl ADR 4468 - 知乎 | duckduckgo |  |  | https://zhuanlan.zhihu.com/p/704175209 |
| 262 | 巴斯夫扩链剂adr-4468和adr-4370怎么用？2026高校实验如何靠它稳定提升熔体强度？ | duckduckgo |  |  | https://bk.taobao.com/k/tezhongsuliao_12436/e5b8142c5a01717006faba63cc37a02e.html |
| 263 | Adr扩链剂 - 百度文库 | duckduckgo |  |  | https://wenku.baidu.com/view/8347c2f000f69e3143323968011ca300a6c3f690.html |